Lab Seminar
Jiapeng Huang
28th, Mar ,2014

---
Outline
- Back Scattering Experiment
- Single Particle Detection Experiment

---
Back Scattering Experiment
From: “Multiple scattering of plasmons at rough surfaces”

---
Back Scattering Experiment
For smooth film there is:
In the presence of multiple scattering, at theta 0 degree Ip/Is is not zero.
From: “Multiple scattering of plasmons at rough surfaces”

---
Back Scattering Experiment
- Measure s and p polarization lights at the back direction (restlight).
- Sputter a 50nm silver layer, with preheating the glass prism to about 300 degree and avoid contacting with metal parts.
xy: plane of incidence
xz: plane of observation

---
Experimental results
Rough film (preheating)
Less rough film (Plasma treating)

---
“Single” nano particle detection
DNA binding
- Hybridization
- High salt environment
- ATPMS binding

---
DNA Binding
ph assistant method(in both citrate and TBE buffer)
- Both surface and particle can be functionalized

---
High salt environment
Put NaCl into DNA-functionalized Au NP(57nm) solution to reach about 200mM concentration.

---
ATPMS binding
- Sputtering ~3nm SiO2 on top of gold.
- Binding ATPMS on the SiO2 surface.
- ATPMS should bind to Au NP
- ATPMS should bind to Carboxylic functionalized particles

---
SEM images
Miguel's 50nm Au particle and nanopartz 57nm Au particle

---
Results
Polymer 0.19 micrometer Carboxylic functionalized
flowing
Not flowing

---
Thank you!